Physicochemical Characterization of a Novel Carbon Nanomaterial: Carbon Dots

Roger M. Leblanc

Department of Chemistry, University of Miami, Coral Gables, FL 33146, USA

Author for correspondence: rml@miami.edu

Carbon dots (CDs) are a group of novel carbon-based spherical nanoparticles (NPs) with diameters less than 10 nm. They are widely present in the nature and can be also synthesized using various carbon-based substances as precursors by either top-down or bottom-up approaches. They are well characterized for tunable surface functionality, excellent photoluminescence (PL), high photostability and water dispersity, good biocompatibility, and nontoxicity. Also, they display different sizes and surface chemistry depending on the preparation methods and precursors applied. Applications of CDs in drug delivery, bioimaging, sensing, and other nanotechnology fields are rapidly rising due to their aforementioned unique properties. In addition, various spectroscopic and microscopic measurements have been performed on diverse CD preparations, which revealed some typical physicochemical features of CDs. For example, UV/vis absorption spectra of CDs usually display two peaks at 250 and 350 nm, which corresponds to C=C and C=O conjugate structures, respectively. Most fluorescence emission spectra have shown an excitation-dependent PL emission of CDs, which arouses a debate regarding the PL mechanism of CDs. The spherical morphologies of different CDs are studied through a combination of atomic force microscopy (AFM) and transmission electron microscopy (TEM) to obtain the three-dimensional data. As for the structural analysis of CDs, Fourier-transform infrared spectroscopy (FTIR), X-ray photoelectron spectroscopy (XPS), Raman spectroscopy, X-ray diffraction (XRD), small-angle X-ray scattering (SAXS), and thermogravimetric analysis (TGA) have all been utilized to investigate the surface functionalities and core structures. Considering the abundant functionalities such as -COOH and -NH2, distinct CDs were conjugated via an amidation reaction mediated by EDC and NHS to explore the construction of large multifunctional carbon-based nanostructures. Also, zeta potential studies show most CDs carry negative charge on the surface, which inspires numerous researches on the electrical or dielectric properties of CDs.

Keywords: Carbon Dots, Physicochemical Characterization, Structure, Conjugation, Dielectric properties.